## Slide 1: Thin film QWRs performance for ALPI-SPES upgrade at INFN-LNL: first results
G. Keppel, on behalf of SRF LNL groups
Link Station Hall Aomori​
October 11-14, 2022

## Slide 2: Outline
Thin film QWR @LNL
  Introduction: ALPI evolution over the years
  The SPES Project @LNL
  ALPI Upgrade for SPES project
  The TANDEM – PIAVE – ALPI Complex
QWR Status @LNL
  Sputtering and Chemistry Facility Upgrade
  Back extrusion cavities
  Results
Conclusion

## Slide 3: Outlook - Introduction
ALPI’s design started in 1990
ALPI started operation in 1994-98 with Pb/Cu technology
Meanwhile from 1993:
  R&D on low b (0,055) 80 MHz bulk Nb resonators (thanks A. Facco)
  R&D on Nb/Cu medium b (0,11) 160 MHz resonators
  (thanks V. Palmieri, S. Stark, A. Porcellato)

## Slide 4: Outlook - Introduction
Nb/Cu resonators are definitively a mainstay of this facility, given the performance and stability over the years.
We have faced a generation transition in the recent years, which has represented a new challenge

## Slide 5: Outlook - Introduction
LNL Nb/Cu experience specially in terms of
Demonstrate the suitability of the technology for large-scale production
ISOLDE - CERN
  Performance
  Stability
  Repeatability
Reliability
  Cost Reduction

## Slide 6: Medium cavity test 2007 -> 2021
Chart: Eacc [MV/m]
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8
1W | 65325115.2495 | 146981509.3113 | 261300460.9979 | 408281970.3092 | 587926037.2452 | 800232661.8059 | 1045201843.9914 | 1322833583.8017 | 1633127881.2366 | 1976084736.2963 | 2351704148.9807 | 2759986119.2899 | 3200930647.2238 | 3674537732.7824 | 4180807375.9657
3W | 21775038.4165 | 48993836.4371 | 87100153.666 | 136093990.1031 | 195975345.7484 | 266744220.602 | 348400614.6638 | 440944527.9339 | 544375960.4122 | 658694912.0988 | 783901382.9936 | 919995373.0966 | 1066976882.4079 | 1224845910.9275 | 1393602458.6552
7W | 9332159.3214 | 20997358.473 | 37328637.2854 | 58325995.7585 | 83989433.8922 | 114318951.6866 | 149314549.1416 | 188976226.2574 | 233303983.0338 | 282297819.4709 | 335957735.5687 | 394283731.3271 | 457275806.7463 | 524933961.8261 | 597258196.5665
15W | 4355007.6833 | 9798767.2874 | 17420030.7332 | 27218798.0206 | 39195069.1497 | 53348844.1204 | 69680122.9328 | 88188905.5868 | 108875192.0824 | 131738982.4198 | 156780276.5987 | 183999074.6193 | 213395376.4816 | 244969182.1855 | 278720491.731
30W | 2177503.8416 | 4899383.6437 | 8710015.3666 | 13609399.0103 | 19597534.5748 | 26674422.0602 | 34840061.4664 | 44094452.7934 | 54437596.0412 | 65869491.2099 | 78390138.2994 | 91999537.3097 | 106697688.2408 | 122484591.0927 | 139360245.8655
FC 40 (2007) | 210953700 | 213200000 | 216500000 | 225000000 | 200000000 | 198000000 | 187500000 | 188700000 | 181870000 | 166300000 | 155900000 | 149000000 | 146000000 | 135600000 | 141000000 | 140900000 | 140192000 | 131398700 | 131307100 | 129300000 | 126300000 | 118780000 | 113256500 | 106728600 | 95356530 | 73346790
FC 40 cavity from CR7
2007 vs. 2021
Same Q0
Same RF performance
Difference at high filed due to low conditioning in 2021

## Slide 7: ALPI-SPES upgrade
Second generation ISOL facility for nuclear physics: Production & re-acceleration of exotic beams
Research and Production of Radio-Isotopes for Nuclear Medicine
Accelerator-based neutron source (Proton and Neutron Facility for Applied Physics)
Cyclotron
ISOL RIBs+
Post-Acc.
Nuclear Applications
Nuclear Medicine
Selective Production of Exotic Species
Notes: Four-leaf clover first phase

## Slide 8: SPES Facility @ LNL
New High power compact CYCLOTRON 70 MeV 750 microA (BEST company)
New configuration of High power ISOL System (8 kW Target ion source)
ALPI superconductive LINAC (up-graded) for RIB’s reacceleration

## Slide 9: INFN-Legnaro: a lab for stable and presently unstable heavy ion beams, and RI production
ISOL1
ISOL2
1+ area
HRMS
cyclotron
CB - MRMS
RFQ
ALPI SC_linac
Applications
ISOL FACILITY and reacceleration
SC_LINAC (ALPI)
XTU Tandem

## Slide 10: SPES layout
ISOL1
ISOL2
Low Energy area
HRMS
Radioisotopes production area (LARAMED)
CYCLOTRON
ISOL bunkers
1/200 mass separator
low energy experimental area
Neutron production area (NEPIR)
RIB reacceleration:
New RT RFQ
ALPI to 10 MeV/A
RIB transfer and selection
1/20.000 mass separator (Beam Cooler + HRMS)
Elettrostatic beam transport
Charge Breeder (n+)
1/1000 mass separator
STABLE BEAM FACILITY

## Slide 11: TANDEM – PIAVE – ALPI complex
SC Linac with 68 QWRs (Nb, Nb/Cu) working @ 4,2 K
in 19 cryostats Veq ~ 48 MeV/q,
beams from 12C to 206Pb,
injected by Tandem or PIAVE
(1994)
SC Linac
ALPI
15 MV VdG Tandem (HV Corp),
H-100Mo beams, E = 30 ÷ 1.5 MeV/A,
CW or pulsed (1984)
Halls 1 and 2
XTU-Tandem
Hall 3
PIAVE
Supernanogan ECR on 350 kV platform
SC-RFQs and QWRs, Veq ~ 8 MV
12C – 206Pb (higher q and Ibeam)
(2006)

## Slide 12: Beam Energies with full SPES Upgrade for Piave-Tandem-ALPI
Chart: 
| 2 | 3 | 2 | 4 | 2.6666666666666665 | 4 | 4.3636363636363633 | 4.4615384615384617 | 3.7647058823529411 | 4.0625 | 4.3529411764705879 | 4.8235294117647056 | 5.6 | 6.4285714285714288 | 4.3809523809523814 | 5.8125 | 8.3333333333333339 | 5.7142857142857144 | 5.0769230769230766 | 5.8461538461538458 | 6.5666666666666664
At present | 22.7 | 16.8 | 22.4 | 11.6 | 17.4 | 11.6 | 11.9 | 10.9 | 12.3 | 13.2 | 12.4 | 11.3 | 8.7 | 8.8 | 9.9 | 8.4 | 6.8 | 8.5 | 9.5 | 8.3 | 7.5
With ALPI in SPES configuration | 28.6 | 19.7 | 28.6 | 14.4 | 23.3 | 14.6 | 13.8 | 13.5 | 16.2 | 18.5 | 16.2 | 14.2 | 10.7 | 10.5 | 13.6 | 10.3 | 8.2 | 10.5 | 11.7 | 10.3 | 9.3

## Slide 13: Matching into ALPI SC linac
Additional 8 cavities
Re-positioned low b cavities
10 MeV/n
for A=130-140
Notes: The superconductive linac ALPI was improved during the years. A refurbishment of the low beta cavities and of the cryogenic system was performed.
An upgrade is going on with the installation of 2 more cryostats to reach the design goal of SPES to have reaccelerated radioactive beams at energies of 10-11 MeV/n

## Slide 14
QWR Status @LNL

## Slide 15: R&D activity for ALPI upgrade
Vacuum systems refurbishing and upgrade:
  QWR and plates sputtering systems.
  Cryostat for off-line test.
Re-definition on coating parameters for Nb/Cu high-β QWRs and plates (for QWR and RFQ) due to:
  Upgrade of the system (new pumps, mass flow implementation, software control, DC and BIAS power supplies etc.).
After > 15 years Nb/Cu with a new team…

## Slide 16: QWR diode sputtering re-engineering
Upgrades started from facility re-modelling using 3D software
Re-engineering of:
Vacuum system.
Vacuum electric connections.
Thermocouple design and connection.
Process gasses.
Control system.
№ | System compound
1 | Niobium cathode
2 | QWR cavity
3 | Titanium ground nets
4 | Copper counter electrode
1
1
1
3D model of the QWR sputtering system: (a) – side view, (b) – bottom view.
Scheme of the QWR diode sputtering system.
2
3
2
2
4
3
3
4
5
(a)
(b)

## Slide 17: QWR diode sputtering system upgrade
Refurbishing of LNL QWR coating system. Major upgrade on:
Vacuum pumps
Ar Mass flow controller
Power supplies (sputtering and BIAS)
Backing controls and cavity heating
NI PLC-PC control System

## Slide 18: Automatic sputtering control and data acquisition

## Slide 19: Tumbling and Chemistry plant upgrade
Tumbling system maintenance
Chemistry plant upgrade (new PLC control system)
New stripping facility
Nb stripping tools
EP facility
EP software
Cavity EP

## Slide 20: QWR Production for CR21 and CR22
8 QWR for ALPI upgrade
4 cavities machined from bulk Cu
 | f0 [MHz] | Δ f0 [MHz]
Reference | 159.390 | 
HB5 | 159.388 | 0.005
HB6 | 159.335 | 0.055
HB7 | 159.328 | 0.062
HB8 | 159.330 | 0.063
Test (DD0) | 159.455 | 0.205
2 cavities back extrusion
Classical production tecnology
Innovative approach

## Slide 21: Cold back extrusion applied to QWR resonators
QWR preformed ready for machining
DD0 test cavity and DD1 produced with this technique

## Slide 22: Cold back extrusion applied to QWR resonators
Back extrusion techniques advantages:
Reduction on copper usage
Surface finishing close to EP finishing
Cheaper machining procedure
  Machining of top and inner part of antenna
  Machining of beam ports
Good material performance
Back extrusion observed disadvantage:
Imperfection on cavity bottom

## Slide 23: Cavity Coating
Sputtering procedure | 
Sputtering pressure [mbar] | 0,08 – 0,2
Cycle time [min] | 15
Number of cycles | 16 – 20
Cathode current [A] | 3,25 – 3,5
Bias voltage [V] | -130
Baking procedure | 
Chamber temperature [°C] | 120 - 220
Substrate temperature [°C] | 400
Baking time [h] | 48 - 96
Nb cathode plasma cleaning
Cavity assembled on coating system
System maintenance
Coated Cavity

## Slide 24: Cavity Plates coating
Procedure | Parameters
Chemical preparation | 
Ultrasound cleaning | In soap solution at 60 °C for 60 min;
Surface activation | In (NH4)2S2O8 solution at 20 ºC for 20 min;
SUBU | SUBU at 72 ºC for 4 – 6 min.
Passivation | H3NO3S for 5 min.
Water rinsing, drying, packaging. | 
Deposition process | 
Baking | Chamber temperature: 100 – 120 °C; Substrate temperature: 300 °C; Time: 48 – 96 hours.
Sputtering | Argon pressure: 0,2 mbar; Cycle time: 6 min; Number of cycles: 10; Substrate temperature: 200 °C; Cathode current: 12 A; Bias voltage: -130 V;
Coated Plates
QWR plates before coating

## Slide 25: QWR antenna delamination
(a)
(b)
(c)
cathode (-800 V)
electrode (-130 V)
net (0 V)
Electric field simulation with QWR – electrode distance: (a) – without electrode; (b) – 40 mm.; (c) – 30 mm.
QWR (-130 V)
Correct positioning of the electrode uniforms electric field distribution in the top antenna area;
Optimal QWR – electrode distance to avoid delamination seems between 30–40 mm.
Delaminated cavity
No delamination

## Slide 26: LNL cavity performance – 160 MHz @4.2K
Chart: Eacc [MV/m]
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8
1W | 65325115.2495 | 146981509.3113 | 261300460.9979 | 408281970.3092 | 587926037.2452 | 800232661.8059 | 1045201843.9914 | 1322833583.8017 | 1633127881.2366 | 1976084736.2963 | 2351704148.9807 | 2759986119.2899 | 3200930647.2238 | 3674537732.7824 | 4180807375.9657
3W | 21775038.4165 | 48993836.4371 | 87100153.666 | 136093990.1031 | 195975345.7484 | 266744220.602 | 348400614.6638 | 440944527.9339 | 544375960.4122 | 658694912.0988 | 783901382.9936 | 919995373.0966 | 1066976882.4079 | 1224845910.9275 | 1393602458.6552
7W | 9332159.3214 | 20997358.473 | 37328637.2854 | 58325995.7585 | 83989433.8922 | 114318951.6866 | 149314549.1416 | 188976226.2574 | 233303983.0338 | 282297819.4709 | 335957735.5687 | 394283731.3271 | 457275806.7463 | 524933961.8261 | 597258196.5665
15W | 4355007.6833 | 9798767.2874 | 17420030.7332 | 27218798.0206 | 39195069.1497 | 53348844.1204 | 69680122.9328 | 88188905.5868 | 108875192.0824 | 131738982.4198 | 156780276.5987 | 183999074.6193 | 213395376.4816 | 244969182.1855 | 278720491.731
30W | 2177503.8416 | 4899383.6437 | 8710015.3666 | 13609399.0103 | 19597534.5748 | 26674422.0602 | 34840061.4664 | 44094452.7934 | 54437596.0412 | 65869491.2099 | 78390138.2994 | 91999537.3097 | 106697688.2408 | 122484591.0927 | 139360245.8655
DD 0 (01.08.2019) | 920143641.3187 | 1321883430.9866 | 1328581500.7396 | 1221594211.8268 | 943233615.9496 | 959333223.1926 | 987518533.8956 | 1024551731.2016 | 1051048758.7327 | 1089752493.046 | 1134993384.567 | 927528749.6165 | 787868969.3558 | 689457685.2581 | 638923368.0071 | 609328223.0012 | 583662036.3707 | 533132214.3847 | 520860703.283 | 488699688.6763 | 455407207.6382 | 436473578.8558 | 432598680.9881 | 401457974.5819 | 390406952.1194 | 360486601.4759 | 341196806.6063 | 329666515.9188 | 295948847.3408 | 291106484.3804 | 713092925.9566 | 727951796.6762 | 768050454.9979 | 794773984.9816 | 825373876.3166 | 846575363.3369 | 902155396.194 | 949734865.5824 | 984040396.3098 | 1007174350.8467 | 1017780370.0132 | 1073925038.2856 | 1102122879.4678 | 1145713397.7794 | 1260694060.5827 | 1299277685.0916 | 1656684922.4696 | 1480752955.6113
HB 7 (13.11.2019) | 819588602.6734 | 548770969.7419 | 430709161.5685 | 348203026.2147 | 300717309.8587 | 277350320.3996 | 256680471.6996 | 233615772.1091 | 222977386.4588 | 195554849.4366 | 178431940.6816 | 157349594.7491 | 142825541.6456 | 133566520.3983 | 121549453.1929 | 112946083.3373 | 104753125.1614 | 96332606.3713
HB 8 (27.02.2020) | 398000000 | 444000000 | 504000000 | 333000000 | 298000000 | 262000000 | 242000000 | 227000000 | 210000000 | 205000000 | 196000000 | 185000000 | 174000000 | 165000000 | 157000000 | 148000000 | 139000000 | 127000000 | 114000000 | 318000000 | 311000000 | 140000000 | 105000000 | 93400000 | 88300000 | 81400000 | 74400000 | 65400000 | 70300000 | 54400000
First cycle RF cold test measurements result.
Cavity № | Q0 | Q [7W] | Eacc [7W], MV/m | Rs, [nΩ]
ALPI Baseline |  | ≥ 1 · 108 | ≥ 4,5 | 
DD 0 | 2,1 · 109 | 4,3 · 108 | 6,5 | 14
HB 7 | 4,5 · 108 | 1,4 · 108 | 3,7 | 90
HB 8 | 1,5 · 108 | 1,4 · 108 | 3,8 | 195
HB 6 | 7,6 · 107 | 6,7 · 107 | 2,6 | 383
HB 5 | 7,6 · 108 | 1,8 · 108 | 5,5 | 38

## Slide 27: LNL cavity performance - 160 MHz @4.2K
Chart: Comparison stripped cavity
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8
1W | 65325115.2495 | 146981509.3113 | 261300460.9979 | 408281970.3092 | 587926037.2452 | 800232661.8059 | 1045201843.9914 | 1322833583.8017 | 1633127881.2366 | 1976084736.2963 | 2351704148.9807 | 2759986119.2899 | 3200930647.2238 | 3674537732.7824 | 4180807375.9657
3W | 21775038.4165 | 48993836.4371 | 87100153.666 | 136093990.1031 | 195975345.7484 | 266744220.602 | 348400614.6638 | 440944527.9339 | 544375960.4122 | 658694912.0988 | 783901382.9936 | 919995373.0966 | 1066976882.4079 | 1224845910.9275 | 1393602458.6552
7W | 9332159.3214 | 20997358.473 | 37328637.2854 | 58325995.7585 | 83989433.8922 | 114318951.6866 | 149314549.1416 | 188976226.2574 | 233303983.0338 | 282297819.4709 | 335957735.5687 | 394283731.3271 | 457275806.7463 | 524933961.8261 | 597258196.5665
15W | 4355007.6833 | 9798767.2874 | 17420030.7332 | 27218798.0206 | 39195069.1497 | 53348844.1204 | 69680122.9328 | 88188905.5868 | 108875192.0824 | 131738982.4198 | 156780276.5987 | 183999074.6193 | 213395376.4816 | 244969182.1855 | 278720491.731
30W | 2177503.8416 | 4899383.6437 | 8710015.3666 | 13609399.0103 | 19597534.5748 | 26674422.0602 | 34840061.4664 | 44094452.7934 | 54437596.0412 | 65869491.2099 | 78390138.2994 | 91999537.3097 | 106697688.2408 | 122484591.0927 | 139360245.8655
DD | 920143641.3187 | 1321883430.9866 | 1328581500.7396 | 1221594211.8268 | 943233615.9496 | 959333223.1926 | 987518533.8956 | 1024551731.2016 | 1051048758.7327 | 1089752493.046 | 1134993384.567 | 927528749.6165 | 787868969.3558 | 689457685.2581 | 638923368.0071 | 609328223.0012 | 583662036.3707 | 533132214.3847 | 520860703.283 | 488699688.6763 | 455407207.6382 | 436473578.8558 | 432598680.9881 | 401457974.5819 | 390406952.1194 | 360486601.4759 | 341196806.6063 | 329666515.9188 | 295948847.3408 | 291106484.3804 | 713092925.9566 | 727951796.6762 | 768050454.9979 | 794773984.9816 | 825373876.3166 | 846575363.3369 | 902155396.194 | 949734865.5824 | 984040396.3098 | 1007174350.8467 | 1017780370.0132 | 1073925038.2856 | 1102122879.4678 | 1145713397.7794 | 1260694060.5827 | 1299277685.0916 | 1656684922.4696 | 1480752955.6113
HB 7 | 357560617.491 | 361549512.8481 | 370638238.2564 | 375423252.3075 | 385003592.6593 | 390695193.5565 | 406401190.2166 | 417216065.6399 | 427300750.9364 | 441834790.0839 | 450206396.6328 | 469453936.4761 | 506430519.6283 | 524000558.0644 | 245877112.026 | 201081464.1132 | 231838177.7899 | 192971598.5268 | 91389558.186 | 101943451.5681 | 119636443.4497 | 126927885.9528 | 135094384.2276 | 152318105.8592 | 162974030.0789 | 164899784.152 | 179689814.0839 | 190059948.0299 | 197975210.3421 | 208516455.7715 | 218688161.202 | 229173992.5426 | 234093494.5806 | 245416494.3295 | 253455960.9048 | 266294034.184 | 273186585.4493 | 284991936.9908 | 318104400.9394 | 95466647.7246 | 60551981.3843 | 46749813.4839
HB 8 | 398000000 | 444000000 | 504000000 | 333000000 | 298000000 | 262000000 | 242000000 | 227000000 | 210000000 | 205000000 | 196000000 | 185000000 | 174000000 | 165000000 | 157000000 | 148000000 | 139000000 | 127000000 | 114000000 | 318000000 | 311000000 | 140000000 | 105000000 | 93400000 | 88300000 | 81400000 | 74400000 | 65400000 | 70300000 | 54400000
DD (stripped) | 1166000000 | 1567000000 | 1666000000 | 1726000000 | 1751000000 | 1668000000 | 1664000000 | 1529000000 | 1485000000 | 1183000000 | 1442000000 | 1409000000 | 118300000 | 75440000 | 113500000 | 138900000 | 177100000 | 179600000 | 202400000 | 231000000 | 273200000 | 262700000 | 314500000 | 384900000 | 445600000 | 325400000 | 495900000 | 608800000 | 662100000 | 768000000 | 897400000 | 1151000000 | 1095000000 | 1046000000 | 956900000 | 903500000 | 1301000000 | 1623000000
HB 7 (stripped) | 145700000 | 143100000 | 140800000 | 138500000 | 126600000 | 123800000 | 121500000 | 119800000 | 129400000 | 130000000 | 127900000 | 125300000 | 125400000 | 121500000 | 122100000 | 121000000 | 119500000 | 114700000 | 107300000 | 106100000 | 105100000 | 104000000 | 102300000 | 100300000 | 96030000 | 90450000 | 86970000 | 82330000 | 77140000 | 70950000 | 65640000 | 58840000 | 54350000 | 50790000 | 46440000 | 41670000 | 39250000 | 34840000 | 33280000 | 33290000 | 29500000 | 27950000 | 143500000 | 147100000 | 160200000 | 164800000 | 154000000 | 156700000 | 154900000 | 149800000 | 133500000 | 133800000
after stripping
7W

## Slide 28: DD back extruded cavity – 160 MHz @4.2K
Chart: Eacc [MV/m]
| 2.0705847097414933 | 2.5824728580484781 | 3.1376678322728 | 3.3339581237514757 | 3.6521681403125665 | 4.0244932789016215 | 4.1793376864251215 | 4.3651758474011668 | 4.5083342294004183 | 4.7484874305581943 | 4.5782350525729836 | 4.6470845558513814 | 4.7818105581966961 | 4.9128433274154357 | 5.0404709011142339 | 5.0088688911436972 | 4.9450590386811974
Before conditioning | 1246527011.0769 | 983965623.9753 | 673297784.2347 | 544557246.4229 | 465370084.1354 | 398791657.4135 | 338386429.6408 | 303096553.8138 | 279774016.6386 | 252353117.0151 | 216071962.8904 | 180945601.5243 | 232040073.7915 | 211674538.8384 | 186901524.909 | 174750098.8081 | 142165706.8042
1W | 65418142.2062 | 147190819.9639 | 261672568.8247 | 408863388.7885 | 588763279.8555 | 801372242.0255 | 1046690275.2987 | 1324717379.6749 | 1635453555.1542 | 1978898801.7365 | 2355053119.422 | 2763916508.2105 | 3205488968.1022 | 3679770499.0969 | 4186761101.1947
3W | 21806047.4021 | 49063606.6546 | 87224189.6082 | 136287796.2628 | 196254426.6185 | 267124080.6752 | 348896758.4329 | 441572459.8916 | 545151185.0514 | 659632933.9122 | 785017706.474 | 921305502.7368 | 1068496322.7007 | 1226590166.3656 | 1395587033.7316
7W | 9345448.8866 | 21027259.9948 | 37381795.5464 | 58409055.5412 | 84109039.9794 | 114481748.8608 | 149527182.1855 | 189245339.9536 | 233636222.1649 | 282699828.8195 | 336436159.9174 | 394845215.4586 | 457926995.4432 | 525681499.871 | 598108728.7421
15W | 4361209.4804 | 9812721.3309 | 17444837.9216 | 27257559.2526 | 39250885.3237 | 53424816.135 | 69779351.6866 | 88314491.9783 | 109030237.0103 | 131926586.7824 | 157003541.2948 | 184261100.5474 | 213699264.5401 | 245318033.2731 | 279117406.7463
30W | 2180604.7402 | 4906360.6655 | 8722418.9608 | 13628779.6263 | 19625442.6619 | 26712408.0675 | 34889675.8433 | 44157245.9892 | 54515118.5051 | 65963293.3912 | 78501770.6474 | 92130550.2737 | 106849632.2701 | 122659016.6366 | 139558703.3732
After conditioning | 1321883430.9866 | 1328581500.7396 | 1221594211.8268 | 943233615.9496 | 959333223.1926 | 987518533.8956 | 1024551731.2016 | 1051048758.7327 | 1089752493.046 | 1134993384.567 | 927528749.6165 | 787868969.3558 | 689457685.2581 | 638923368.0071 | 609328223.0012 | 583662036.3707 | 533132214.3847 | 520860703.283 | 488699688.6763 | 455407207.6382 | 436473578.8558 | 432598680.9881 | 401457974.5819 | 390406952.1194 | 360486601.4759 | 341196806.6063 | 329666515.9188 | 295948847.3408 | 291106484.3804 | 713092925.9566 | 727951796.6762 | 768050454.9979 | 794773984.9816 | 825373876.3166 | 846575363.3369 | 902155396.194 | 949734865.5824 | 984040396.3098 | 1007174350.8467 | 1017780370.0132 | 1073925038.2856 | 1102122879.4678 | 1145713397.7794 | 1260694060.5827 | 1299277685.0916 | 1656684922.4696 | 1480752955.6113 | 147476302.1769

## Slide 29: Sputtering parameters vs QWR performance
Q vs. sputtering pressure
Q vs. electrode distance
Chart: Sputtering pressure, [mbar]
| 0.2 | 0.09 | 0.1 | 0.08 | 0.15 | 0.15 | 0.08 | 0.1 | 7.4999999999999997E-2
DD 0 [1] HB 7 [1] HB 8 [1] HB 6 [1] HB 5 [1] DD 0 [2] HB 7 [2] HB 8 [2] HB 6 [2] | 2100000000 | 450000000 | 150000000 | 76000000 | 760000000 | 1000000000 | 140000000 | 300000000 | 92000000
Chart: Counter electrode - QWR inner conductor distance, [mm]
| 40 | 25 | 30 | 25 | 35 | 30 | 25 | 35 | 20
DD 0 [1] HB 7 [1] HB 8 [1] HB 6 [1] HB 5 [1] DD 0 [2] HB 7 [2] HB 8 [2] HB 6 [2] | 2100000000 | 450000000 | 150000000 | 76000000 | 760000000 | 1000000000 | 140000000 | 300000000 | 92000000

## Slide 30: Conclusions
A major refurbishment of the sputtering systems and cavity tests facility were carried out at LNL.
Improvements and upgrades were made in substrate preparation (mechanical and chemical).
Intense R&D was carried out so to redefine the deposition parameters necessary to obtain cavities respecting ALPI requirements.
3 cavities (of the 8 needed) were ready to be installed in the cryostats
the back extrusion technique for cavity production was explored and proved to be efficient, cost-effective and promising.

## Slide 31: Special thanks
… to the LNL coating group and RF LNL service: O. Azzolini, G. Bisoffi, D. Bortolato, E. Chyhyrynets, E. Fagotti, E. Munaron, C. Pira, F. Stivanello, A. Tsymbaliuk.

## Slide 32
Thanks​ for your attention
keppel@lnl.infn.it