## Slide 1: High Q/G Beta 0.53 HWR Cavity R&D Program for High Gradient Cryomodule to Enhance Operational Gradient Margin
K. Saito MSU/FRIB SRF Development Manager
TTC Meeting at Aomori, Oct. 11 – 14, 2022
High Q/G R&D, W1

## Slide 2: FRIB Cavity Performance Limits
Figure 1: Statistics of cavity performance in the vertical test on the FRIB 0.53 HWRs.
Type | QWR-0.041 | QWR-0.085 | HWR-0.29 | HWR-0.53
Total number of certificated cavities | 16 | 106 | 72 | 148
1. Quench < Bp=85 MT | 1 (0.6%) | 0 (0%) | 13 (18%) | 2 (0.1%)
2. Field emission X-ray below Bp=85 mT | 3 (19%) | 41(39%) | 21 (29%) | 109 (74%)
3. Pure HFQS, including quench > Bp=85 mT | 9 (56%) | 26 (25%) | 32 (44%) | 21 (14%)
4. Suspicious HFQS X-ray onset > Bp=85 mT | 3 (19%) | 39 (37%) | 6 (8%) | 16 (11%)
HFQS total (3+4) | 12 (75%) | 65 (61%) | 38 (53%) | 37 (25%)
Table 1: Statistics of the field limitation with all the cavities, in FRIB production
Cavity field limitation on FRIB production cavities is mostly FE or HFQS.
Limitation: FE 19 - 74%, and HFQS 75 - 25%.
Recent data analysis shows Qo loading at below X-ray 100 mR/hr could be due to HFQS. HFQS limitation should be much higher than 75-25%.
Remind, FRIB cavities are processed by BCP, and heated at 600 OC for 10 hr.
0.53 HWR
C. Zhang et. al., Nucl. Inst. and Method.
https://doi.org/10.1016/i.nima.2021.165675

## Slide 3: R&D Project Narrative DOE R&D Project, $704k, 2 years
FRIB maintenance:
stable and reliable machine operation for user service
Replacement of degraded cryomodules
e.g. 0.53HWR spare cryomodule
Enough performance margin for the future cavity degradation in the replaced CM itself
HighQ/G Spare Cryomodule
Current FRIB cavity operation,
5 - 7.5 MV/m with Qo ~ 1E+10
HFQS is the fundamental Q/G limitation with FRIB cavities
Development of transformative processing technology, for High Q/G performance,
Eacc > 10 MV/m @ Qo > 2E+10,
for FRIB 0.53 spare cryomodule
Story
Objective
Spare cryomodule opera-table Eacc > 10 MV/m @ Qo >1.5E+10

## Slide 4: Object 1: Transformative Technology against FE or HFQS on FRIB Cavities: Electropolishing
Electropolishing (EP) produces a smooth surface.
  Typical surface roughness: EP ~ 1-2 mm, BCP ~ 5 mm.
This smooth surface makes easy to rinsing, and results in less FE.
Successful pilot study result of EP with 162.5MHZ beta = 0.11 HWR at ANL
EP+ LTB could eliminate the HFQS, and results in High Q?G performance.
The goal is promising and low risk in technical development.
Figure 2: Electropolishing on 162.5 MHz b= 0.11 HWRs at ANL. LTB was not carried out, therefore EP-HFQS is observed slightly at Bop > 85 mT These cavies reached 17 - 28 MV/m with a rather flat Qo. Bp/Eacc = 5.02 mT/ [MV/m].
Z. A Conway et.al. SRF2015
https://accelconf.web.cern.ch/srf2015/papers/weba05.pdf
EP only, no LTB
TTC meeting in Aomori, Japan, WG1, Oct. 11-14, 2022, Saito

## Slide 5: EP System at FRIB
EP system (horizontally rotating EP system) has been constructed at FRIB for future high gradient cavities, i.e. energy upgrade 644 MHz elliptical cavities.
Commissioning is under way, utilizing 0.53HWRs.
Fig.3: EP system at FRIB, which is located SRF Highbay.

## Slide 6: Object 1: EP or EP+LTB Expected Cavity Performance in these processing
Fig.4: Expected Cavity Performance in Object 1, EP or EP+LTB.
Required Qo performance
FRIB operation
High Q/G performance is expected by EP or EP+LTB with low technical risk.

## Slide 7: Object 2: Strengthen magnetic shielding Backup Plan for High Qo Performance
EP or EP+LTB could be limited in high Q performance.
If reduced the remnant field in VT Dewar below 10-5 mG (current ~ 20 mG), Qo performance could be improved.
Put on magnetic local magnetic shield around the helium Jacket, which is developed for FRIB production cavities.
Fig.5: Expected Cavity Performance by EP or EP+LTB + an additional local magnetic shield.

## Slide 8: Object 3: Challenge to A Transformative BCP HFQS-free BCP(combined LTB)
If similar high Q/G performance as EP is achieved by BCP, it could lead a big benefit to low/medium beta and reflecting mod cavities which have a complicate geometry.
However, so far, BCP based on the mixture: HF, HNO3, and H3PO4 can not remove the HFQS even taken the post BCP LTB (120OC, 48hr), with fine grain cavities (not heated 800-900 OC).
MSU PhD activity (Didi, 2015-2019) concluded that it is due to the reaction of nitric acid, If add nitric acid in the current EP acid, a HFQS not removed by LTB appears (reminded in KEK data).
The PhD activity successfully developed a new BCP acid without nitric acid, which can produce surface finishing ~ 3 mm with small samples (Didi Luo, PhD thesis, MSU, 2019 Aug.)
The object 3 tests this new BCP acid on the 0.53HWR and investigate the VT cavity performance.
Fig. 6: If added HNO3 acid the current EP mixture, HFQS not removed by LTB appears (PhD thesis, Didi Luo, Aug. 2019). Reminded from KEK data by PhD activities, by T. Higuchi, 2001.

## Slide 9: Object 4: Challenge to Much Higher Qo Performance New doping technology
Expected the success of High Q/G cavity performance for 0.53HWR by EP, or combination of LTB and strengthening magnetic shielding.
However, needs more Qo performance for a much higher G operation, Eacc > 12 MV/m.
Object 4 explores new doping technologies.
  Current doping technology: N-doping or Oxygen doping, cavities are annealed at 800 - 900 OC high temperature in a vacuum furnace before the doping process.
  Such a high temperature annealing could have a big risk to the already dressed a He tank (titanium) FRIB 0.53 spare HWRs, i.e. frequency tuning point of view.
  Investigate whether the high temperature annealing is essential for doping.
  New doping method without high temperature annealing will be explored.

## Slide 10: Summary
Recently, FRIB has been awarded a R&D project from DOE with a budget $704k and 2 years since 2022 September, in order to develop transformative processing technology for High Q/G performance, for FRIB 0.53 spare cryomodule.
In this project, EP or EP+LTB will applied to realize the high Q/G performance for FRIB 0.53HWRs, which is well developed on ILC cavities and low technical risk.
Local magnetic shield will be added around cavity jacket to reduce remnant magnetic field in VT Dewar, which has been developed in the FRIB production cavities, and well works.
After that, two challenges will be done with high risk:
  Development of HFQS-free BCP
  New doping method without high temperature annealing.
This presentation showed just a project plan, but the result will be reported in future TTC meeting step by step.