## Slide 1: Low temperature co-sputtering of Nb3Sn thin films on copper
Márton Major, Nils Schäfer, Alexey Arzumanov, Hamidreza Ghasemi and Lambert Alff
Department of Materials Science, Advanced Thin Film Technology Group, Technical University of Darmstadt, Germany

## Slide 2
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 3
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 4
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 5
Nb-Sn phase diagram
Charlesworth JP, Macphail I, Madsen PE. Experimental work on the niobium-tin constitution diagram and related studies. Journal of Materials Science. 1970 Jul 1;5(7):580-603.

## Slide 6
Challenge: Vapor-pressure of Sn

## Slide 7
Process routes of thermal Nb3Sn synthesis
Nb
Nb3Sn
Nb
Sn
Nb
Sn
Nb
Sn
Nb
800 – 1200 °C
+ 3 – 24 h
Nb
Nb3Sn
Single target sputtering (amorphous Nb3Sn on Nb, oxides,…)
Multilayer sputtering (Nb/Sn layers on Nb, oxides,…)
Tin sputtering, tin evaporation, … (Sn layers on Nb)

## Slide 8
TUDa approach: Nb3Sn co-sputtering
Nb
Nb3Sn
Sn Target
Nb Target
Argon
Heater
MFC
Butterfly valve
Substrate
Exhaust

## Slide 9
Nb3Sn roadmap
Optimization of the sputtering parameters (sputter power, substrate temperature, etc.) on fused silica substrate
Adaptation of the growth parameters (further optimization of growth temperature etc.) for copper substrate
Upscaling of the sputtering process to the cavity geometry

## Slide 10
Optimization of growth parameters on fused silica substrate

## Slide 11
Stoichiometry vs power ratio
Tin content measured by EDX plotted as a function of Nb dc magnetron
sputtering power input. Substrate was kept at room temperature. The stoichiometric tin content in Nb3Sn of 25% is marked by the line.
N. Schäfer et al, J. Appl. Phys. 128, 133902 (2020); https://doi.org/10.1063/5.0015376

## Slide 12
Stoichiometry vs temperature at PNb/PSn = 5.25 (optimized)
Tin content measured by EDX plotted as a function of substrate temperature
at a fixed power ratio of 5.25. The stoichiometric tin content in Nb3Sn of
25% is marked by the dashed line.
N. Schäfer et al, J. Appl. Phys. 128, 133902 (2020); https://doi.org/10.1063/5.0015376
(20W Sn / 105W Nb)

## Slide 13
XRD: Temperature Study

## Slide 14
Secondary electron images [(a) and (b)] of sputtered Nb3Sn thin films at a fixed substrate temperature of 435 °C and a power ratio of 5.25, while the power input is increased from 15 W Sn/79W Nb (a) to 30 W Sn/158 W Nb (b).
Nb3Sn morphology on fused silica substrate

## Slide 15
R-T measurements as function of substrate temperature and power input

## Slide 16
Comparison of the voltage versus current pattern of two sputtered Nb3Sn thin films measured at 4 K. The power input was increased from 15W Sn/79W Nb to 30W Sn/158W Nb while the substrate temperature during growth was fixed to 320 ◦C for both samples. The external field applied during the IV measurement was increased from 0 mT to 200 mT.
N. Schäfer et al., unpublished
Possible role of grain boundaries (weak links)

## Slide 17
Optimization of growth parameters on copper substrate

## Slide 18
< 520 °C @ 60 min.
growth
Direct growth of Nb3Sn on copper

## Slide 19
Increasing thickness beneficial for critical temperature
Tc,0=16.8 K @ 480 °C!
120 nm < λ (140 nm), still shielding
Performance as a function of Nb3Sn film thickness

## Slide 20
Bulk performance for 700 nm thickness.
Below 700 nm enhancement of Hc1 (known below λ=140 nm)
Decreasing film thickness beneficial for Hc1
Performance as a function of Nb3Sn film thickness

## Slide 21
Trade-off between Tc and Hc1
Performance as a function of Nb3Sn film thickness

## Slide 22
Adhesion test: scratch test
Measurements by Sebastian Bruns

## Slide 23
Pop-In: Cracking of the layer
Adhesion test: nano ball indentation
Measurements by Sebastian Bruns

## Slide 24
Upscaling to copper cavities

## Slide 25
Sputter chamber for cavity and small samples

## Slide 26
Tungsten heating wire
Magnetrons
Sample stage
Double wall shield
Sputtering system

## Slide 27
Sputtering system

## Slide 28
Sputtering spot
Cavity sputtering

## Slide 29
Acknowledgement
Thank you for your attention!
Funded by BMBF Project 05H21RDRB1 and the German Research Foundation (DFG) through grant GRK2128 (AccelencE)
Jürgen Schreeck
Nail Karabas
Stefan Petzold
Sara Amidi
Sebastian Bruns (PhM)
Norbert Pietralla Michaela Arnold