## Slide 1
Cristian Pira
Nb3Sn on Cu coating by Magnetron Sputtering from Target Synthesized via Liquid Tin Diffusion
Aomori
October 11-14, 2022
On behalf of INFN LNL SRF group
CSN5 INFN experiment
i.FAST has received funding from the European Union’s Horizon 2020 programme under GA No 101004730.

## Slide 2: Outline
Project goal and motivations
Liquid Tin Diffusion technique introduction
Target production first results
First sputtering test with LTD target

## Slide 3: Goal and motivations

## Slide 4: Goal
Produce and test a Nb3Sn on Cu 6 GHz elliptical cavity
Nb on Cu 6 GHz cavity
Motivations:
Cu is a cheaper substrate
Higher thermal conductivity (important also for applications beyond high energy physics with cryocooler cooling )
6 GHz are a good test bench (handable, cheap, fast to test, test facility ready @LNL)

## Slide 5: LNL Strategy
Use the same Magnetron Sputtering configuration of Nb on Cu 6 GHz elliptical cavity
Nb on Cu 6 GHz cavity coating system
Replace Nb Cylindrical target with a Nb3Sn one
Not so easy because Nb3Sn is extremely brittle!
Sintered bulk target cannot be used

## Slide 6: Nb3Sn on Cu LNL strategy for 6 GHz cavities
Dipping in Liquid Tin
+ Annealing
Nb target
Magnetron Sputtering
Nb3Sn on Nb target

## Slide 7: Liquid Tin Diffusion in a couple of slides…

## Slide 8: Vapor or Liquid Tin Diffusion
Tin Vapor Diffusion
Liquid Tin Diffusion (Dipping)
Similar principle: Sn diffuse onto Nb and react at High T
Both suitable to growth Nb3Sn films on Nb substrates
Liquid Tin diffusion allows coating of thick films
Notes: Nikuman (ravioli pieni di carne)

## Slide 9: Liquid Tin Diffusion Set Up @
System designed in 2005 for the coating of 6 GHz elliptical cavities
UHV Inconel chamber
2 Separate resistive furnaces
Nb sample

## Slide 10: Dipping process (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006
Lower
Furnace
(Liquid Tin)
Upper Furnace (Annealing Zone)
Cooling
zone
furnace
heating
∼1 h
furnaces heating
annealing
in Sn vapor
dipping
annealing
cooling
1000 °C
1000 °C
30 °C
Sample temperature
ΔT ∼ - 100-150 °C
Temperature furnaces profile

## Slide 11: Dipping process (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006
Lower
Furnace
(Liquid Tin)
Upper Furnace (Annealing Zone)
Cooling
zone
furnace
heating
∼1 h
dipping
0.5 h
Temperature furnaces profile
furnaces heating
annealing
in Sn vapor
dipping
annealing
cooling
1000 °C
1000 °C
30 °C

## Slide 12: Dipping process (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006
Lower
Furnace
(Liquid Tin)
Upper Furnace (Annealing Zone)
Cooling
zone
furnace
heating
∼1 h
dipping
0.5 h
Temperature furnaces profile
furnaces heating
annealing
in Sn vapor
dipping
2 h
annealing
in Sn vapor
annealing
cooling
1000 °C
1000 °C
30 °C

## Slide 13: Dipping process (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006
Lower
Furnace
(Liquid Tin)
Upper Furnace (Annealing Zone)
Cooling
zone
furnace
heating
∼1 h
dipping
0.5 h
Temperature furnaces profile
furnaces heating
annealing
in Sn vapor
dipping
2 h
annealing
in Sn vapor
annealing
5 h
annealing
cooling
400 °C
1000 °C
30 °C

## Slide 14: Dipping process (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006
Lower
Furnace
(Liquid Tin)
Upper Furnace (Annealing Zone)
Cooling
zone
furnace
heating
∼1 h
dipping
0.5 h
Temperature furnaces profile
furnaces heating
annealing
in Sn vapor
dipping
2 h
annealing
in Sn vapor
annealing
5 h
annealing
cooling
∼ 1 h
cooling

## Slide 15: Results (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006 S. M. Deambrosis, SRF 2009
Good performance on planar samples
Poor performance on 6 GHz cavity
6 GHz @ 4.2 K
QBCS Nb = 3 * 107
Sn drop
Nb3Sn

## Slide 16: Results (LNL 2006)
S. M. Deambrosis et al., “A15 superconductors: An alternative to niobium for RF cavities,” Physica C, 2006 S. M. Deambrosis, SRF 2019
cavity
droplets of Sn
Sn
External surface
Internal surface
Drops of unreacted Tin on the surface
Sn
Nb3Sn
Sn
Spurius phases

## Slide 17: Dipping process optimization and Nb3Sn target production

## Slide 18: Dipping Optimized Process
nucleation
Nb2O5
Nb
Nb3Sn
3 h
cooling
Temperature furnaces profile
nucleation
600 °C
1000 °C
30 °C
M. Zanierato, SRF 2021
Nucleation improved adding a vapor coating step
on anodized Nb samples

## Slide 19: Dipping Optimized Process
Vapor
coating
nucleation
Nb2O5
Nb
Nb3Sn
3 h
2 h
cooling
Temperature furnaces profile
nucleation
Vapor
coating
1000 °C
1000 °C
30 °C
M. Zanierato, SRF 2021
Nucleation improved adding a vapor coating step
on anodized Nb samples

## Slide 20: Dipping Optimized Process
Vapor
coating
nucleation
Nb2O5
Nb
Nb3Sn
3 h
2 h
cooling
Temperature furnaces profile
nucleation
Vapor
coating
dipping
3 h
dipping
1000 °C
1000 °C
30 °C
M. Zanierato, SRF 2021

## Slide 21: Dipping Optimized Process
Vapor
coating
nucleation
Nb2O5
Nb
Nb3Sn
3 h
2 h
cooling
Temperature furnaces profile
nucleation
Vapor
coating
dipping
3 h
dipping
annealing
in Sn vapor
6 h
1000 °C
1000 °C
30 °C
Vapor
annealing
M. Zanierato, SRF 2021

## Slide 22: Dipping Optimized Process
Vapor
coating
nucleation
Nb2O5
Nb
Nb3Sn
3 h
2 h
cooling
Temperature furnaces profile
nucleation
Vapor
coating
dipping
3 h
dipping
annealing
in Sn vapor
6 h
annealing
15 h
annealing
400 °C
1000 °C
30 °C
Vapor
annealing
M. Zanierato, SRF 2021

## Slide 23: Dipping Optimized Process
Vapor
coating
nucleation
Nb2O5
Nb
Nb3Sn
3 h
2 h
cooling
Temperature furnaces profile
nucleation
Vapor
coating
dipping
3 h
dipping
annealing
in Sn vapor
6 h
Vapor
annealing
annealing
15 h
annealing
cooling
1 h
M. Zanierato, SRF 2021

## Slide 24: Test with 1” target
Shape optimized
to collect and remove Tin excess
Anodized samples
Nb3Sn coated samples
1’’ Magnetron ready

## Slide 25: Dipping time - thickness
100 μm  ∼ 63 hours of dipping!
Nb3Sn growing rate by dipping is related to the Sn diffusion in Nb and can be described by Fick’ laws of diffusion
x: Nb3Sn thickness
t: dipping time
k: a costant that takes in account the diffusion coefficient D
35 μm
25 μm
14 μm
30 μm
24 hours of dipping  ∼ 62 μm
C. Pira, Thin Films Workshop SRF 2021
M. Zanierato, SRF 2021
in progress

## Slide 26: Target Morphology (SEM + EDS characterization)
Stoichiometric Nb-Sn composition
Chromium contamination (10-20% on surface) Ni and Fe are also present
XRD shows only Nb3Sn phase

## Slide 27: Target cross section
35 μm
Nb
Nb3Sn
resin
Contamination is superficial
No contamination in Sn crucible
Main candidate for Cr contamination:
Vacuum chamber made by Inconel Alloy
EDS profile

## Slide 28: Tin content modulation
Vapor annealing step can be used to modulate Tin content
With Vapor Annealing Step
Without Vapor Annealing Step

## Slide 29: Target surface
∼6 microns eroded
700 nm coated
Center: Sn 23.5%
Race Track: Sn 22.8%
Ext. border: Sn 23.0%
Race Track side: Sn 23.2%

## Slide 30: First sputtering test on Quartz
1” target prepared by Dipping (30 microns thick)
Coating on quartz samples by MS
  I = 0.1 A (5 mA/cm2)
  t = 30 min
  T = 750 °C
Process stopped when V started to decrease
Zanierato et al,
SRF Proceedings 2021

## Slide 31: First sputtering test on Quartz
Good composition
No Cr visible by EDS
Cracks due to Quartz substrate
No Tc measured
2 New targets ready for new tests

## Slide 32: Solution to Cr contamination
Inconel chamber replaced by a Nb chamber produced at Zanon

## Slide 33: New problems have come…
Nb is not stable as Inconel at high T in air
After the first test (30 min @ 1000 °C)
a very thick film of Nb2O5 growth on the external surface
We tested several solutions without success:
Nb anodization
High T paints
Allumina by HVOF
We are redesigning the system with inductive heating and a double chamber to avoid oxidation of Nb chamber

## Slide 34: Conclusions
Proved the possibility of realizing targets via LTD
Easy modulation of target thickness and Tin content
Two main aspect to optimize:
Chromium poisoning
Study the magnetron sputtering deposition parameters
in progress with commercial sintered Nb3Sn targets

## Slide 35: Take home message
Quartz
Sapphire
Copper
Do not use quartz for temperatures above 550 C!

## Slide 36: Thanks to the LNL INFN team: Alessandro Salmaso, Davide Ford, Luca Torrassa, Eduard Chyhyrynets, Fabrizio Stivanello, Giorgio Keppel, Oscar Azzolini
Special thanks to Vanessa Garcia Diaz
Open postdoc position @LNL:
(deadline October 30th)
https://l.infn.it/job
cristian.pira@lnl.infn.it

## Slide 37: Thanks for your attention
cristian.pira@lnl.infn.it
Work supported by the INFN CSN5
i.FAST has received funding from the European Union’s Horizon 2020 Research and Innovation programme under GA No 101004730.

## Slide 38: Backup slides

## Slide 39
How does the new process work in RF?

## Slide 40: How does the new process work in RF?
Process has been adapted to reduce Nb3Sn thickness
(5-10 microns as the old cavities)
Vapor
coating
dipping
annealing
in Sn vapor
annealing
cooling
nucleation
9 h
9 h
0.5 h
7.5 h
15 h
1 h

## Slide 41: 6 GHz cavity #1 (only geometry test)
First test in a broken cavity to test possible geometry effect
No tin drops!
Very good surface
5-10 micron Nb3Sn thickness

## Slide 42: Cr-Ni contamination in 6 GHz cavity
Inner Surface of a 6 GHz elliptical cavity
Nb 65% Sn 35% Cr 0%
The cavity geometry preserves the inner surface from contamination
External Surface of a 6 GHz elliptical cavity
Nb 42% Sn 13% Cr 38% Ni 7.2%

## Slide 43: 6 GHz cavity #1 (only geometry test)
(200)
(210)
(211)
(320)
(420)
(421)
(321)
(400)
(222)
Inner Surface XRD of a 6 GHz elliptical cavity
XRD shows only the Nb3Sn phase

## Slide 44: 6 GHz cavity #2
Same process of cavity #1
Problem with upper furnace: annealing at 920 °C instead of 940 °C
45 h of annealing instead of 15 h
Metallic tin outside
Dark spots in the inner surface
(signs of tin excess)

## Slide 45: Tc and RF Test
Flux expulsion measured by a Flux Gate placed in the equator
Tc ∼ 11.5 K
Poor RF performances comparable to old process
(Sn excess? Cr-Ni contamination? Thick film?)
6 GHz @ 4.2 K
QBCS Nb = 3 * 107