## Slide 1
Mechanical Polishing of Nb3Sn Thin Films
Presenter: Eric Viklund (NU/FNAL)
Contributors: D. N. Seidman (NU),
D. Burk, S. Posen (FNAL)

## Slide 2: Nb3Sn Thin Film Created by Sn-Vapor Deposition
Nb3Sn cavities produced by Sn-vapor deposition
  Nb cavities are coated by a microcrystalline thin film
  Typically, 2-3μm thick
Resulting in a matte surface finish
  Microscopic surface roughness
  Grain faceting
  Thermal etching at grain boundaries
S. Posen, Ph.D. Thesis, Cornell University (2015).
4 μm

## Slide 3: Impact of Surface Roughness on Nb3Sn SRF Cavity Performance
Surface roughness has been shown to cause a localized increase in magnetic field.[1]
Up to 60% stronger fields in some regions.
Nb3Sn coated cavities produced at Fermilab reach a record accelerating gradient.[2]
Films are thinner and smoother than previous coatings
  Up to 24 MV/m accelerating gradient
Further removal of surface roughness could lead to accelerating fields in the 30-40 MV/m range.
2. S Posen et al 2021 Supercond. Sci. Technol. 34 025007
Shiny thin film coating
1. R. Porter, D. L. Hall, M. Liepe, J. T. Maniscalco, Proc. Linac Conference 2016, MOPRC027 (2016).
60% Field Enhancement

## Slide 4: Reviewing Polishing Methods for Nb3Sn SRF Cavities.
Further reduction in surface roughness requires a method for polishing Nb3Sn films.
Two main options are available:
Chemical polishing:
  Chemical polishing does not work well on Nb3Sn.
Mechanical polishing:
  Only limited attempts to mechanical polish Nb3Sn films have been tried.
Is mechanical polishing a good alternative for polishing Nb3Sn SRF cavities?
Pudasaini, Uttar, et al. Proceedings of the 18th International Conference on RF Superconductivity,(Lanzhou, China). 2017.
Hu, H. Conference on RF Superconductivity. 2019.

## Slide 5: Centrifugal Barrel Polishing
Centrifugal barrel polishing (CBP) was developed to mechanically polish SRF cavities.
Cavities are filled with polishing media
Cavities are rotated at 120 RPM in the barrel polishing machine
Rotating motion pushes polishing media against the cavity surface

## Slide 6: Nb3Sn Sample Polishing Using a Coupon Cavity
This experiment is performed using Nb3Sn samples barrel polished in a coupon cavity.
By using a coupon cavity samples are exposed to realistic polishing conditions
Nb3Sn cavities must be destroyed for microstructural analysis of the surface
Dozens of small Nb3Sn samples can be coated at once and analyzed before and after polishing treatments
Minimize trial-and-error for finding polishing parameters
Internal View

## Slide 7: Abrasive Finishing Materials
Only the final nano-polishing step is applied.
Only fine-grit materials
The cavity is filled with two materials:
Nanoparticle abrasive suspension
Solid substrate to carry abrasive
Nanoparticle suspensions tested:
40nm silicate particles
50nm alumina particles
Solid substrates tested:
0.25” wooden balls
0.5” felt cubes

## Slide 8: Surface Profile after Progressing Amounts of Mechanical Polishing
86 μm
0 hours
2 hours
4 hours
6 hours
8 hours

## Slide 9: Scanning Electron Microscopy of Mechanically Polished Nb3Sn Films
Initial Surface
2 hours
4 hours
6 hours
8 hours
5 μm
5 μm
5 μm
5 μm
5 μm

## Slide 10: Mechanical Polishing Improves Surface Roughness With Minimal Material Removal
Cross-section analysis using scanning electron microscopy shows film thickness.
Material removed per hour of polishing
~170 nm when using felt
~95 nm when using wood
Chart: Tumbling Duration in Hours
| 0 | 2 | 4 | 6 | 8
Felt Cubes | 3.104 | 2.796 | 2.876 | 1.952 | 1.826
Wooden Spheres | 3.241 | 3.184 | 2.518

## Slide 11: Surface Roughness of Mechanically Polished Nb3Sn Films
Mirror-like surface finish
10x reduction in surface roughness after 8 hours of tumbling
As-coated Nb3Sn
Nb3Sn after polishing
Pudasaini, Uttar, et al. Proceedings of the 18th International Conference on RF Superconductivity,(Lanzhou, China). 2017.
Chart: Duration of Centrifugal Barrel Polishing [hours]
| 0 | 2 | 4 | 6 | 8 | 10
Shiny Nb3Sn Films | 63 | 63 | 63 | 63 | 63 | 63
Polished Nb3Sn | 208.2381 | 185.1343 | 100.2737 | 54.2454 | 16.5368
Electropolished Nb | 25 | 25 | 25 | 25 | 25 | 25
Mechanical Polishing
Electropolishing

## Slide 12: Surface Damage Caused by Wooden Spheres
Scratches
Cracks
Damaged layer
Samples polished with felt media show no surface damage.
Platinum Layer
Oxide Layer
Nb3Sn
Damaged Layer

## Slide 13: Ultrasonic Cleaning
Ultrasonic cleaning removes residual abrasive particles.
Most particles gone after two hours
Some particles remain in crevices
No surface damage caused by ultrasonic cleaning
Before Cleaning
After Cleaning (2hrs)
Before Ultrasonic Cleaning
Platinum Layer
Nb3Sn
Oxide Layer
After Ultrasonic Cleaning
Platinum Layer
Nb3Sn
Oxide Layer

## Slide 14: Applying the Polishing Procedure to a Nb3Sn SRF Cavity
Mechanical polishing was tested on a Nb3Sn-coated single cell 1.3GHz cavity
4 hours of centrifugal barrel polishing
30 minutes of cleaning in an ultrasonic cleaner
Rinsed with a high-pressure (100 bars) water jet
Before Coating
After Coating
After Polishing

## Slide 15: Performance of a Mechanically Polished Nb3Sn SRF Cavity
The accelerating field and quality factor of the cavity was measured after mechanical polishing.
Cavity performance was degraded after CBP.
40% reduction in maximum accelerating field
Severe Q-slope
Possible causes include:
Residual alumina particles and other contaminants
Surface damage caused by barrel polishing
Exposed sub-surface film defects
Chart: Accelerating Field [MV/m]
| 3.16321064 | 3.12667502 | 2.3052539799999998 | 2.2998050999999999 | 2.4722664000000001 | 1.8353171699999999 | 1.53823373 | 1.3265123700000001 | 2.4294928100000002 | 2.7311534100000001 | 2.9791048600000001 | 3.05326824 | 3.21010551 | 3.3585187699999999 | 3.5121741100000001 | 3.5487984799999999 | 1.93110122 | 1.66965119 | 1.48851453 | 1.2942389299999999 | 1.31135318 | 1.1089264299999999 | 0.91064886199999995 | 0.83913228900000003 | 0.73211455400000003 | 3.3882260199999998 | 3.6906140000000001 | 3.97417709 | 4.1236569799999998 | 4.36377141 | 4.4790761899999998 | 4.6480257099999998 | 4.7230781400000001 | 4.8820916600000004 | 4.7095892900000003 | 4.7095861799999996 | 4.7774500099999999 | 4.7179403500000001 | 4.6066310000000001 | 4.4685677999999998 | 4.4238068899999998 | 4.1425641400000002 | 4.6674362599999997 | 3.8038277900000002 | 3.6772194100000002 | 3.8125339199999999 | 3.20056056 | 2.8415431999999998 | 2.4111515200000002 | 2.4432802499999999 | 2.2895918100000001 | 2.1223857800000001 | 1.8627126899999999 | 1.38719342 | 1.2271149100000001 | 1.08301512 | 0.90280830199999995 | 0.72475121099999995
4.4K After CBP | 8888103050 | 6124229210 | 11562833800 | 15134986100 | 26790143800 | 14748894300 | 14214412400 | 12809013500 | 12374153200 | 10621486300 | 9997664290 | 7873096380 | 6230390840 | 5653022900 | 4982955190 | 4855981510 | 13770187000 | 14555745500 | 15075026000 | 16048949100 | 15454593300 | 16371005300 | 16620094400 | 16718867300 | 17153334000 | 5390979330 | 4345842820 | 3185101230 | 2785249360 | 2128848540 | 1714609750 | 1193970430 | 1042184260 | 749205156 | 493896754 | 444171324 | 621914290 | 712920846 | 848299685 | 1114382760 | 1249446520 | 1940479700 | 2471535870 | 2618332770 | 3069214360 | 3272904330 | 4238431800 | 6511286750 | 7424318600 | 7601897300 | 7723080620 | 8054398830 | 8480470790 | 9471353580 | 9651469290 | 9940289670 | 10659994800 | 10488475200
4.4K Before CBP | 23143361800 | 17876552000 | 22694270600 | 23161525600 | 23730945600 | 23545774900 | 23279796400 | 22994580600 | 22515254300 | 21903820100 | 21280212000 | 20123231400 | 19384594500 | 18477556300 | 16851239400 | 15837371900 | 15081005700 | 14631380100 | 14035298100 | 13713888500 | 13340831400 | 13150935800 | 17112939300 | 12719182900 | 13003548000 | 12464559200 | 12062238800 | 11700599800 | 11185132700 | 10200146600 | 10167109800 | 9840167550 | 9408361320 | 9019511540 | 8879178480 | 7209223780 | 8913762610 | 7953843030 | 7814778150 | 7696339690 | 7454509490 | 7012311440 | 6979552200
2.0K Before CBP | 45095644400 | 46484829700 | 71461836000 | 85445202800 | 88339240400 | 88541070400 | 92012738500 | 99301364300 | 91030691000 | 96299315700 | 98262788800 | 103191781000 | 92831887500 | 87943381400 | 87230858700 | 90657287300 | 90988377100 | 89840295000 | 84925707300 | 87256408100 | 87564657200 | 88745309200 | 88992755600 | 83874114800 | 85064715700 | 79181977900 | 79282055600 | 72817731700 | 63959415800 | 63442611100 | 63542541500 | 56005029700 | 48550250000 | 40455401300 | 40440659500 | 40475072600 | 34124321000 | 30777565200 | 27640917800 | 25152986900 | 23528166800 | 22279459200 | 21231285100 | 20177108700 | 19142780900 | 18115254600 | 17491373800 | 17375644400 | 17432706600
Typical Nb Q at 4K

## Slide 16: Future Research Directions
Determining the cause of performance degradation.
  More cavity testing
  Heat mapping
  Cavity cut-out analysis
Improving post-polishing cleaning.
  Improving ultrasonic and high-pressure rinsing procedures
  Exploring chemical cleaning methods
Characterizing the Nb3Sn surface after mechanical polishing.
  Surface damage
  Surface stoichiometry
  Oxide film
Repairing the surface after polishing by recoating the surface.
  Perform a short additional coating cycle of Nb3Sn after polishing to fill in damaged areas

## Slide 17: Key Findings
Using mechanical polishing we can obtain a smooth Nb3Sn surface, comparable to electropolished niobium.
The performance of the mechanically polished cavity was degraded.
Further studies will be done to analyze the cavity surface after mechanical polishing.
86 μm
0 hours
2 hours
4 hours
6 hours
8 hours
Chart: Tumbling Duration in Hours
| 0 | 2 | 6 | 8
 | 3.104 | 2.796 | 1.952 | 1.826
As-coated Nb3Sn
Nb3Sn after polishing
Chart: Duration of Centrifugal Barrel Polishing [hours]
| 0 | 2 | 4 | 6 | 8 | 10
Shiny Nb3Sn Films | 63 | 63 | 63 | 63 | 63 | 63
Polished Nb3Sn | 208.2381 | 185.1343 | 100.2737 | 54.2454 | 16.5368
Electropolished Nb | 25 | 25 | 25 | 25 | 25 | 25